0001

| Pat Munro (Alness) Ltd Caplich Quarry Alness Ross-shire IV17 0XO 0001 |  |  |  |
| --- | --- | --- | --- |
| EN 12620 Aggregates for Concrete From Dornoch Sand and Gravel 10/20. 4/10 |  |  |  |
| Particle Shape |  |  | FI35 |
| Particle size |  |  | 4/10 10/20 Gc 85/15 |
| Particle Density | Saturated Surface Dry | Declared | 2.61 Mg/m3 |
|  | Oven Dry | Declared | 2.59 Mg/m3 |
|  | Apparent | Declared | 2.67 Mg/m3 |
| Cleanliness |  |  |  |
|  | Fines Content | Category | F4 |
|  | Shell content | Category | SC10 |
| Resistance to fragmentation |  | Category | LA30 |
| Resistance to Polishing |  | Declared | PSV55 |
| Resistance to Abrasion |  | Category | AAVNR |
| Resistance to wear |  | Category | MDE10 |
| Composition /Content |  |  |  |
|  | Composition of recycled | Category | NR |
|  | Chlorides | Declared | <0.001% |
|  | Acid Soluble Sulfates | Declared | <0.1 |
|  | Total sulfur | Declared | 0.01 |
|  | Carbonate Content | Category | NR |
|  | Influence on initial setting time of cement (recycled) | Category | ANR |
| Volume Stability |  |  |  |
|  | Dry shrinkage | Declared | Pass 0.036 |
| Water Absorption |  | Category | WA24 1 |
| Durability against freeze-thaw |  | Declared | WA24 1 MSSV18 |
| Emission of Radioactivity | Threshold | Value | NR |
| Release of Heavy metals | Threshold | Value | NR |
| Release of Polyaromatic carbons | Threshhold | Value | NR |
| Durability against ASR |  | Declared | Normal |

Issue No 0001									                          Issue Date May 2016